Supplementary Table S1: Representative and complete EMPA analyses of Cr-spinels from the Kağızman Ophiolite chromitites. Structural formulae were calculated on the basis of 32 oxygens. Abbreviations: Chr = chromitite; MgChr = magnesiochromitite; Hc = hercynite; Spl = spinel; Mt = magnetite.

| Sample Id |  | ST 4X_1 |  | ST 4X_2 |  | ST 4X_3 |  | ST 4X_4 |  | ST 4X_5 |  | ST 4X_6 |  | ST 4X_7 |  | ST 4X_8 |  | ST 4X_9 |  | ST 4X_10 |  | ST 4X_11 |  | ST 4X_12 |  | ST 4X_13 |  | ST 4X_14 |  | ST 4X_15 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cr2O3 |  | 55.33 |  | 49.73 |  | 51.71 |  | 52.63 |  | 59.35 |  | 53.37 |  | 50.02 |  | 55.53 |  | 49.87 |  | 50.53 |  | 55.30 |  | 50.63 |  | 55.93 |  | 58.85 |  | 52.23 |  |
| Al2O3 |  | 13.46 |  | 18.67 |  | 14.97 |  | 16.90 |  | 11.35 |  | 14.93 |  | 19.52 |  | 14.37 |  | 18.77 |  | 17.03 |  | 15.10 |  | 17.96 |  | 15.01 |  | 11.89 |  | 17.95 |  |
| TiO2 |  | 0.32 |  | 0.44 |  | 0.36 |  | 0.31 |  | 0.41 |  | 0.45 |  | 0.41 |  | 0.44 |  | 0.33 |  | 0.26 |  | 0.30 |  | 0.24 |  | 0.33 |  | 0.26 |  | 0.24 |  |
| FeO |  | 18.14 |  | 16.99 |  | 18.20 |  | 16.11 |  | 17.51 |  | 17.24 |  | 16.53 |  | 17.97 |  | 16.85 |  | 18.62 |  | 18.16 |  | 18.84 |  | 17.80 |  | 18.73 |  | 17.92 |  |
| MgO |  | 12.21 |  | 13.49 |  | 14.28 |  | 13.30 |  | 11.04 |  | 13.18 |  | 13.37 |  | 11.10 |  | 14.06 |  | 13.03 |  | 10.53 |  | 11.92 |  | 10.85 |  | 10.37 |  | 11.02 |  |
| MnO |  | 0.34 |  | 0.35 |  | 0.32 |  | 0.34 |  | 0.31 |  | 0.57 |  | 0.46 |  | 0.34 |  | 0.25 |  | 0.32 |  | 0.47 |  | 0.22 |  | 0.24 |  | 0.25 |  | 0.22 |  |
| NiO |  | 0.32 |  | 0.34 |  | 0.21 |  | 0.46 |  | 0.26 |  | 0.30 |  | 0.14 |  | 0.25 |  | 0.18 |  | 0.54 |  | 0.35 |  | 0.38 |  | 0.49 |  | 0.37 |  | 0.53 |  |
| Total |  | 100.12 |  | 100.01 |  | 100.05 |  | 100.05 |  | 100.22 |  | 100.03 |  | 100.45 |  | 99.99 |  | 100.31 |  | 100.33 |  | 100.22 |  | 100.19 |  | 100.65 |  | 100.72 |  | 100.11 |  |
| Cr |  | 1.399 |  | 1.222 |  | 1.281 |  | 1.304 |  | 1.527 |  | 1.334 |  | 1.222 |  | 1.413 |  | 1.217 |  | 1.249 |  | 1.406 |  | 1.259 |  | 1.414 |  | 1.511 |  | 1.309 |  |
| Al |  | 0.507 |  | 0.684 |  | 0.553 |  | 0.624 |  | 0.435 |  | 0.556 |  | 0.711 |  | 0.545 |  | 0.683 |  | 0.628 |  | 0.572 |  | 0.666 |  | 0.566 |  | 0.455 |  | 0.670 |  |
| Ti |  | 0.008 |  | 0.010 |  | 0.008 |  | 0.007 |  | 0.010 |  | 0.011 |  | 0.010 |  | 0.011 |  | 0.008 |  | 0.006 |  | 0.007 |  | 0.006 |  | 0.008 |  | 0.006 |  | 0.006 |  |
| Fe3+ |  | 0.077 |  | 0.074 |  | 0.149 |  | 0.057 |  | 0.017 |  | 0.089 |  | 0.049 |  | 0.021 |  | 0.085 |  | 0.110 |  | 0.008 |  | 0.064 |  | 0.005 |  | 0.021 |  | 0.009 |  |
| Fe2+ |  | 0.408 |  | 0.368 |  | 0.328 |  | 0.365 |  | 0.459 |  | 0.367 |  | 0.378 |  | 0.463 |  | 0.350 |  | 0.377 |  | 0.481 |  | 0.432 |  | 0.471 |  | 0.488 |  | 0.466 |  |
| Mg |  | 0.582 |  | 0.625 |  | 0.667 |  | 0.621 |  | 0.536 |  | 0.621 |  | 0.616 |  | 0.532 |  | 0.647 |  | 0.607 |  | 0.505 |  | 0.559 |  | 0.517 |  | 0.502 |  | 0.521 |  |
| Mn |  | 0.009 |  | 0.009 |  | 0.008 |  | 0.009 |  | 0.008 |  | 0.015 |  | 0.012 |  | 0.009 |  | 0.007 |  | 0.008 |  | 0.013 |  | 0.006 |  | 0.006 |  | 0.007 |  | 0.006 |  |
| Ni |  | 0.008 |  | 0.008 |  | 0.005 |  | 0.012 |  | 0.007 |  | 0.008 |  | 0.003 |  | 0.006 |  | 0.004 |  | 0.014 |  | 0.009 |  | 0.010 |  | 0.013 |  | 0.010 |  | 0.014 |  |
| Total |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  |
| Mg# |  | 0.59 |  | 0.63 |  | 0.67 |  | 0.63 |  | 0.54 |  | 0.63 |  | 0.62 |  | 0.54 |  | 0.65 |  | 0.62 |  | 0.51 |  | 0.56 |  | 0.52 |  | 0.51 |  | 0.53 |  |
| Cr# |  | 0.73 |  | 0.64 |  | 0.70 |  | 0.68 |  | 0.78 |  | 0.71 |  | 0.63 |  | 0.72 |  | 0.64 |  | 0.67 |  | 0.71 |  | 0.65 |  | 0.71 |  | 0.77 |  | 0.66 |  |
| Fe3+# |  | 0.04 |  | 0.04 |  | 0.08 |  | 0.03 |  | 0.01 |  | 0.04 |  | 0.02 |  | 0.01 |  | 0.04 |  | 0.06 |  | 0.00 |  | 0.03 |  | 0.00 |  | 0.01 |  | 0.00 |  |
| Al# |  | 0.26 |  | 0.35 |  | 0.28 |  | 0.31 |  | 0.22 |  | 0.28 |  | 0.36 |  | 0.28 |  | 0.34 |  | 0.32 |  | 0.29 |  | 0.33 |  | 0.29 |  | 0.23 |  | 0.34 |  |
| Al2O3Melt |  | 12.52 |  | 14.22 |  | 13.07 |  | 13.70 |  | 11.62 |  | 13.06 |  | 14.45 |  | 12.86 |  | 14.25 |  | 13.74 |  | 13.11 |  | 14.02 |  | 13.08 |  | 11.87 |  | 14.02 |  |
| TiO2melt |  | 0.45 |  | 0.57 |  | 0.49 |  | 0.44 |  | 0.54 |  | 0.59 |  | 0.54 |  | 0.57 |  | 0.46 |  | 0.38 |  | 0.43 |  | 0.35 |  | 0.45 |  | 0.38 |  | 0.36 |  |
| Fe2+# |  | 0.41 |  | 0.37 |  | 0.33 |  | 0.37 |  | 0.46 |  | 0.37 |  | 0.38 |  | 0.46 |  | 0.35 |  | 0.38 |  | 0.49 |  | 0.44 |  | 0.48 |  | 0.49 |  | 0.47 |  |
| FeO/MgOmelt |  | 1.19 |  | 1.11 |  | 1.02 |  | 1.04 |  | 1.25 |  | 1.07 |  | 1.12 |  | 1.35 |  | 1.05 |  | 1.21 |  | 1.46 |  | 1.38 |  | 1.39 |  | 1.43 |  | 1.45 |  |
| Chr (mol%) |  | 29.73 |  | 23.41 |  | 22.41 |  | 24.76 |  | 35.78 |  | 25.75 |  | 23.83 |  | 33.38 |  | 22.13 |  | 24.91 |  | 34.61 |  | 28.10 |  | 34.01 |  | 37.67 |  | 31.14 |  |
| MgChr |  | 42.45 |  | 39.80 |  | 45.63 |  | 42.13 |  | 41.72 |  | 43.61 |  | 38.79 |  | 38.42 |  | 40.94 |  | 40.18 |  | 36.33 |  | 36.38 |  | 37.33 |  | 38.78 |  | 34.83 |  |
| Hc (mol%) |  | 10.78 |  | 13.10 |  | 9.67 |  | 11.85 |  | 10.20 |  | 10.74 |  | 13.86 |  | 12.88 |  | 12.42 |  | 12.52 |  | 14.08 |  | 14.86 |  | 13.61 |  | 11.34 |  | 15.95 |  |
| Spl (mol%) |  | 15.39 |  | 22.27 |  | 19.69 |  | 20.17 |  | 11.89 |  | 18.18 |  | 22.56 |  | 14.82 |  | 22.97 |  | 20.19 |  | 14.79 |  | 19.24 |  | 14.94 |  | 11.68 |  | 17.85 |  |
| Mt (mol%) |  | 1.64 |  | 1.42 |  | 2.61 |  | 1.08 |  | 0.41 |  | 1.72 |  | 0.95 |  | 0.50 |  | 1.55 |  | 2.20 |  | 0.19 |  | 1.43 |  | 0.11 |  | 0.52 |  | 0.23 |  |
| Species |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  |
| ST 4X_16 | ST 4X_17 |  | ST 4X_18 |  | ST 4X_19 |  | ST 4X_20 |  | ST 4X_21 |  | ST 4X_22 |  | ST 4X_23 |  | ST 4X_24 |  | ST 4X_25 |  | ST 4X_26 |  | ST 4X_27 |  | ST 4X_28 |  | ST 4X_29 |  | ST 4X_30 |  | ST 4X_31 |  |
| 47.98 | 50.62 |  | 58.64 |  | 50.38 |  | 48.64 |  | 49.97 |  | 52.69 |  | 49.27 |  | 50.63 |  | 52.78 |  | 59.86 |  | 49.89 |  | 50.35 |  | 52.86 |  | 50.87 |  | 51.27 |  |
| 17.47 | 18.24 |  | 11.56 |  | 17.40 |  | 17.51 |  | 18.36 |  | 16.95 |  | 16.49 |  | 15.61 |  | 17.45 |  | 10.48 |  | 17.82 |  | 18.84 |  | 17.16 |  | 17.97 |  | 18.15 |  |
| 0.28 | 0.37 |  | 0.30 |  | 0.32 |  | 0.35 |  | 0.27 |  | 0.34 |  | 0.44 |  | 0.21 |  | 0.34 |  | 0.28 |  | 0.23 |  | 0.31 |  | 0.31 |  | 0.28 |  | 0.28 |  |
| 18.99 | 18.35 |  | 18.43 |  | 19.02 |  | 18.72 |  | 18.66 |  | 18.21 |  | 18.75 |  | 17.27 |  | 17.28 |  | 18.69 |  | 18.11 |  | 18.92 |  | 18.25 |  | 18.10 |  | 16.73 |  |
| 14.86 | 12.16 |  | 10.71 |  | 12.36 |  | 14.24 |  | 12.27 |  | 11.08 |  | 14.31 |  | 15.62 |  | 11.68 |  | 10.09 |  | 13.28 |  | 10.81 |  | 10.98 |  | 12.14 |  | 13.01 |  |
| 0.22 | 0.22 |  | 0.25 |  | 0.27 |  | 0.21 |  | 0.32 |  | 0.38 |  | 0.26 |  | 0.29 |  | 0.28 |  | 0.41 |  | 0.39 |  | 0.44 |  | 0.33 |  | 0.30 |  | 0.24 |  |
| 0.42 | 0.31 |  | 0.13 |  | 0.38 |  | 0.41 |  | 0.34 |  | 0.52 |  | 0.43 |  | 0.46 |  | 0.35 |  | 0.33 |  | 0.35 |  | 0.43 |  | 0.42 |  | 0.43 |  | 0.39 |  |
| 100.23 | 100.27 |  | 100.02 |  | 100.13 |  | 100.08 |  | 100.18 |  | 100.17 |  | 99.96 |  | 100.10 |  | 100.17 |  | 100.14 |  | 100.07 |  | 100.10 |  | 100.31 |  | 100.09 |  | 100.07 |  |
| 1.170 | 1.255 |  | 1.513 |  | 1.252 |  | 1.192 |  | 1.237 |  | 1.324 |  | 1.213 |  | 1.239 |  | 1.319 |  | 1.557 |  | 1.230 |  | 1.258 |  | 1.327 |  | 1.264 |  | 1.266 |  |
| 0.635 | 0.674 |  | 0.445 |  | 0.645 |  | 0.640 |  | 0.678 |  | 0.635 |  | 0.605 |  | 0.569 |  | 0.650 |  | 0.406 |  | 0.655 |  | 0.702 |  | 0.642 |  | 0.666 |  | 0.668 |  |
| 0.007 | 0.009 |  | 0.007 |  | 0.007 |  | 0.008 |  | 0.006 |  | 0.008 |  | 0.010 |  | 0.005 |  | 0.008 |  | 0.007 |  | 0.005 |  | 0.007 |  | 0.007 |  | 0.007 |  | 0.007 |  |
| 0.183 | 0.054 |  | 0.027 |  | 0.089 |  | 0.151 |  | 0.072 |  | 0.025 |  | 0.160 |  | 0.182 |  | 0.015 |  | 0.023 |  | 0.104 |  | 0.025 |  | 0.016 |  | 0.057 |  | 0.053 |  |
| 0.307 | 0.427 |  | 0.476 |  | 0.411 |  | 0.334 |  | 0.416 |  | 0.459 |  | 0.328 |  | 0.265 |  | 0.441 |  | 0.492 |  | 0.369 |  | 0.475 |  | 0.468 |  | 0.419 |  | 0.384 |  |
| 0.683 | 0.568 |  | 0.521 |  | 0.579 |  | 0.658 |  | 0.573 |  | 0.525 |  | 0.665 |  | 0.721 |  | 0.550 |  | 0.495 |  | 0.617 |  | 0.509 |  | 0.520 |  | 0.569 |  | 0.606 |  |
| 0.006 | 0.006 |  | 0.007 |  | 0.007 |  | 0.005 |  | 0.008 |  | 0.010 |  | 0.007 |  | 0.008 |  | 0.007 |  | 0.011 |  | 0.010 |  | 0.012 |  | 0.009 |  | 0.008 |  | 0.006 |  |
| 0.010 | 0.008 |  | 0.003 |  | 0.010 |  | 0.010 |  | 0.009 |  | 0.013 |  | 0.011 |  | 0.011 |  | 0.009 |  | 0.009 |  | 0.009 |  | 0.011 |  | 0.011 |  | 0.011 |  | 0.010 |  |
| 3.000 | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  | 3.000 |  |
| 0.69 | 0.57 |  | 0.52 |  | 0.58 |  | 0.66 |  | 0.58 |  | 0.53 |  | 0.67 |  | 0.73 |  | 0.55 |  | 0.50 |  | 0.63 |  | 0.52 |  | 0.53 |  | 0.58 |  | 0.61 |  |
| 0.65 | 0.65 |  | 0.77 |  | 0.66 |  | 0.65 |  | 0.65 |  | 0.68 |  | 0.67 |  | 0.69 |  | 0.67 |  | 0.79 |  | 0.65 |  | 0.64 |  | 0.67 |  | 0.66 |  | 0.65 |  |
| 0.09 | 0.03 |  | 0.01 |  | 0.04 |  | 0.08 |  | 0.04 |  | 0.01 |  | 0.08 |  | 0.09 |  | 0.01 |  | 0.01 |  | 0.05 |  | 0.01 |  | 0.01 |  | 0.03 |  | 0.03 |  |
| 0.32 | 0.34 |  | 0.22 |  | 0.32 |  | 0.32 |  | 0.34 |  | 0.32 |  | 0.31 |  | 0.29 |  | 0.33 |  | 0.20 |  | 0.33 |  | 0.35 |  | 0.32 |  | 0.34 |  | 0.34 |  |
| 13.88 | 14.10 |  | 11.72 |  | 13.85 |  | 13.89 |  | 14.14 |  | 13.72 |  | 13.58 |  | 13.29 |  | 13.87 |  | 11.21 |  | 13.98 |  | 14.27 |  | 13.78 |  | 14.02 |  | 14.07 |  |
| 0.41 | 0.50 |  | 0.43 |  | 0.44 |  | 0.48 |  | 0.39 |  | 0.47 |  | 0.57 |  | 0.32 |  | 0.47 |  | 0.40 |  | 0.35 |  | 0.43 |  | 0.44 |  | 0.40 |  | 0.40 |  |
| 0.31 | 0.43 |  | 0.48 |  | 0.42 |  | 0.34 |  | 0.42 |  | 0.47 |  | 0.33 |  | 0.27 |  | 0.45 |  | 0.50 |  | 0.37 |  | 0.48 |  | 0.47 |  | 0.42 |  | 0.39 |  |
| 1.06 | 1.33 |  | 1.35 |  | 1.32 |  | 1.11 |  | 1.34 |  | 1.44 |  | 1.08 |  | 0.88 |  | 1.31 |  | 1.43 |  | 1.17 |  | 1.58 |  | 1.46 |  | 1.31 |  | 1.13 |  |
| 19.49 | 27.58 |  | 36.65 |  | 26.90 |  | 21.32 |  | 26.76 |  | 31.36 |  | 21.42 |  | 17.92 |  | 29.72 |  | 39.30 |  | 23.91 |  | 30.79 |  | 31.81 |  | 27.44 |  | 25.13 |  |
| 43.35 | 36.70 |  | 40.13 |  | 37.86 |  | 42.00 |  | 36.83 |  | 35.84 |  | 43.40 |  | 48.78 |  | 37.04 |  | 39.56 |  | 40.03 |  | 33.01 |  | 35.31 |  | 37.26 |  | 39.64 |  |
| 10.58 | 14.81 |  | 10.77 |  | 13.85 |  | 11.44 |  | 14.66 |  | 15.03 |  | 10.69 |  | 8.24 |  | 14.64 |  | 10.25 |  | 12.73 |  | 17.17 |  | 15.39 |  | 14.45 |  | 13.26 |  |
| 23.53 | 19.71 |  | 11.79 |  | 19.49 |  | 22.54 |  | 20.18 |  | 17.18 |  | 21.66 |  | 22.42 |  | 18.25 |  | 10.32 |  | 21.31 |  | 18.41 |  | 17.09 |  | 19.62 |  | 20.92 |  |
| 3.04 | 1.19 |  | 0.66 |  | 1.90 |  | 2.71 |  | 1.57 |  | 0.59 |  | 2.83 |  | 2.63 |  | 0.34 |  | 0.57 |  | 2.01 |  | 0.61 |  | 0.39 |  | 1.24 |  | 1.05 |  |
| MgChr | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  | MgChr |  |

| ST 4X_32 | ST 4X_33 | ST 4X_34 | ST 4X_35 | ST 4X_36 | ST 4X_37 | ST 4X_38 | ST 4X_39 | ST 4X_40 | ST 4X_41 | ST 4X_42 | ST 4X_43 | ST 4X_44 | ST 4X_45 | ST 4X_46 | LB 4_1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 48.76 | 48.96 | 48.82 | 49.64 | 49.95 | 50.44 | 49.60 | 50.83 | 52.65 | 56.94 | 46.68 | 46.86 | 42.31 | 58.86 | 55.52 | 60.42 |
| 18.36 | 17.05 | 17.40 | 18.70 | 17.90 | 18.65 | 18.63 | 17.89 | 17.86 | 13.92 | 21.75 | 20.69 | 23.15 | 13.35 | 15.43 | 11.16 |
| 0.24 | 0.38 | 0.41 | 0.34 | 0.23 | 0.24 | 0.28 | 0.26 | 0.28 | 0.30 | 0.31 | 0.32 | 0.55 | 0.34 | 0.51 | 0.38 |
| 19.68 | 19.26 | 18.81 | 17.52 | 18.83 | 16.96 | 18.58 | 18.15 | 16.61 | 17.95 | 17.35 | 16.95 | 15.77 | 14.45 | 14.60 | 15.41 |
| 12.24 | 13.74 | 13.89 | 13.06 | 12.35 | 13.02 | 12.39 | 12.33 | 12.13 | 10.84 | 13.47 | 14.50 | 17.54 | 13.16 | 13.60 | 12.36 |
| 0.21 | 0.37 | 0.35 | 0.40 | 0.41 | 0.31 | 0.34 | 0.32 | 0.33 | 0.30 | 0.29 | 0.34 | 0.28 | 0.29 | 0.35 | 0.48 |
| 0.54 | 0.43 | 0.38 | 0.50 | 0.41 | 0.38 | 0.50 | 0.48 | 0.39 | 0.37 | 0.41 | 0.46 | 0.51 | 0.23 | 0.38 | 0.21 |
| 100.04 | 100.20 | 100.07 | 100.16 | 100.08 | 100.00 | 100.32 | 100.27 | 100.26 | 100.62 | 100.26 | 100.13 | 100.11 | 100.68 | 100.39 | 100.42 |
| 1.209 | 1.205 | 1.201 | 1.221 | 1.239 | 1.244 | 1.224 | 1.260 | 1.308 | 1.446 | 1.131 | 1.133 | 0.992 | 1.475 | 1.378 | 1.539 |
| 0.679 | 0.626 | 0.638 | 0.686 | 0.662 | 0.685 | 0.686 | 0.661 | 0.662 | 0.527 | 0.785 | 0.745 | 0.809 | 0.499 | 0.571 | 0.424 |
| 0.006 | 0.009 | 0.010 | 0.008 | 0.005 | 0.006 | 0.007 | 0.006 | 0.007 | 0.007 | 0.007 | 0.007 | 0.012 | 0.008 | 0.012 | 0.009 |
| 0.102 | 0.151 | 0.142 | 0.077 | 0.088 | 0.060 | 0.077 | 0.067 | 0.017 | 0.012 | 0.070 | 0.107 | 0.174 | 0.010 | 0.027 | 0.019 |
| 0.414 | 0.351 | 0.347 | 0.379 | 0.406 | 0.382 | 0.408 | 0.409 | 0.420 | 0.470 | 0.374 | 0.326 | 0.217 | 0.373 | 0.356 | 0.397 |
| 0.572 | 0.638 | 0.644 | 0.606 | 0.578 | 0.605 | 0.577 | 0.576 | 0.568 | 0.519 | 0.615 | 0.661 | 0.776 | 0.622 | 0.637 | 0.594 |
| 0.006 | 0.010 | 0.009 | 0.011 | 0.011 | 0.008 | 0.009 | 0.008 | 0.009 | 0.008 | 0.008 | 0.009 | 0.007 | 0.008 | 0.009 | 0.013 |
| 0.014 | 0.011 | 0.010 | 0.013 | 0.010 | 0.010 | 0.013 | 0.012 | 0.010 | 0.010 | 0.010 | 0.011 | 0.012 | 0.006 | 0.010 | 0.005 |
| 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 |
| 0.58 | 0.65 | 0.65 | 0.62 | 0.59 | 0.61 | 0.59 | 0.58 | 0.58 | 0.52 | 0.62 | 0.67 | 0.78 | 0.63 | 0.64 | 0.60 |
| 0.64 | 0.66 | 0.65 | 0.64 | 0.65 | 0.64 | 0.64 | 0.66 | 0.66 | 0.73 | 0.59 | 0.60 | 0.55 | 0.75 | 0.71 | 0.78 |
| 0.05 | 0.08 | 0.07 | 0.04 | 0.04 | 0.03 | 0.04 | 0.03 | 0.01 | 0.01 | 0.04 | 0.05 | 0.09 | 0.01 | 0.01 | 0.01 |
| 0.34 | 0.32 | 0.32 | 0.35 | 0.33 | 0.34 | 0.35 | 0.33 | 0.33 | 0.27 | 0.40 | 0.38 | 0.41 | 0.25 | 0.29 | 0.21 |
| 14.14 | 13.75 | 13.85 | 14.23 | 14.00 | 14.22 | 14.21 | 14.00 | 13.99 | 12.69 | 15.02 | 14.76 | 15.34 | 12.47 | 13.23 | 11.54 |
| 0.36 | 0.51 | 0.54 | 0.47 | 0.35 | 0.35 | 0.40 | 0.38 | 0.41 | 0.42 | 0.44 | 0.45 | 0.69 | 0.47 | 0.65 | 0.51 |
| 0.42 | 0.35 | 0.35 | 0.38 | 0.41 | 0.39 | 0.41 | 0.42 | 0.42 | 0.48 | 0.38 | 0.33 | 0.22 | 0.37 | 0.36 | 0.40 |
| 1.40 | 1.17 | 1.14 | 1.18 | 1.32 | 1.15 | 1.32 | 1.29 | 1.22 | 1.37 | 1.20 | 1.06 | 0.82 | 0.89 | 0.91 | 0.97 |
| 26.31 | 22.68 | 22.25 | 24.27 | 26.41 | 24.66 | 26.13 | 26.85 | 28.11 | 34.71 | 22.02 | 19.57 | 11.81 | 27.94 | 25.26 | 31.29 |
| 36.31 | 41.28 | 41.33 | 38.79 | 37.56 | 39.04 | 36.92 | 37.81 | 38.06 | 38.36 | 36.19 | 39.63 | 42.13 | 46.64 | 45.10 | 46.82 |
| 14.77 | 11.77 | 11.82 | 13.63 | 14.11 | 13.59 | 14.63 | 14.09 | 14.22 | 12.65 | 15.30 | 12.88 | 9.63 | 9.45 | 10.46 | 8.62 |
| 20.39 | 21.43 | 21.96 | 21.78 | 20.06 | 21.52 | 20.67 | 19.84 | 19.25 | 13.98 | 25.13 | 26.08 | 34.36 | 15.77 | 18.69 | 12.90 |
| 2.21 | 2.84 | 2.64 | 1.53 | 1.87 | 1.19 | 1.64 | 1.42 | 0.36 | 0.29 | 1.36 | 1.85 | 2.07 | 0.20 | 0.49 | 0.38 |
| MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr |

| LB 4_2 | LB 4_3 | LB 4_4 | LB 4_5 | LB 4_6 | LB 4_7 | LB 4_8 | LB 4_9 | LB 4_10 | LB 4_11 | LB 4_12 | LB 4_13 | LB 4_14 | LB 4_15 | LB 4_16 | LB 4_17 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 60.14 | 58.06 | 60.85 | 54.85 | 53.21 | 48.12 | 50.51 | 48.70 | 45.86 | 62.26 | 54.77 | 46.11 | 45.98 | 46.31 | 49.86 | 53.38 |
| 11.51 | 13.06 | 11.07 | 16.28 | 16.75 | 20.07 | 18.81 | 19.85 | 21.42 | 8.96 | 15.63 | 22.09 | 21.58 | 21.38 | 19.45 | 16.86 |
| 0.32 | 0.64 | 0.31 | 0.37 | 0.37 | 0.36 | 0.39 | 0.32 | 0.20 | 0.40 | 0.35 | 0.39 | 0.37 | 0.28 | 0.29 | 0.31 |
| 15.65 | 15.18 | 15.82 | 16.33 | 16.62 | 17.90 | 16.91 | 16.82 | 18.98 | 17.23 | 16.79 | 17.48 | 17.94 | 16.61 | 16.59 | 16.96 |
| 11.93 | 12.49 | 11.90 | 12.08 | 12.47 | 12.86 | 12.82 | 13.69 | 13.10 | 10.52 | 12.59 | 13.41 | 13.54 | 14.90 | 13.34 | 11.73 |
| 0.46 | 0.56 | 0.33 | 0.34 | 0.30 | 0.38 | 0.39 | 0.35 | 0.27 | 0.65 | 0.36 | 0.28 | 0.26 | 0.19 | 0.24 | 0.39 |
| 0.31 | 0.36 | 0.39 | 0.27 | 0.32 | 0.33 | 0.27 | 0.39 | 0.45 | 0.33 | 0.26 | 0.37 | 0.46 | 0.46 | 0.28 | 0.45 |
| 100.32 | 100.35 | 100.67 | 100.51 | 100.04 | 100.02 | 100.10 | 100.14 | 100.28 | 100.36 | 100.75 | 100.13 | 100.13 | 100.13 | 100.05 | 100.08 |
| 1.536 | 1.467 | 1.553 | 1.369 | 1.327 | 1.180 | 1.245 | 1.188 | 1.114 | 1.623 | 1.363 | 1.117 | 1.115 | 1.113 | 1.222 | 1.337 |
| 0.438 | 0.492 | 0.421 | 0.606 | 0.623 | 0.734 | 0.691 | 0.722 | 0.776 | 0.348 | 0.580 | 0.798 | 0.780 | 0.766 | 0.711 | 0.630 |
| 0.008 | 0.015 | 0.008 | 0.009 | 0.009 | 0.008 | 0.009 | 0.008 | 0.005 | 0.010 | 0.008 | 0.009 | 0.009 | 0.006 | 0.007 | 0.007 |
| 0.010 | 0.010 | 0.011 | 0.007 | 0.032 | 0.069 | 0.045 | 0.075 | 0.101 | 0.009 | 0.041 | 0.068 | 0.088 | 0.108 | 0.054 | 0.018 |
| 0.413 | 0.396 | 0.416 | 0.424 | 0.406 | 0.395 | 0.396 | 0.359 | 0.386 | 0.466 | 0.401 | 0.380 | 0.372 | 0.315 | 0.377 | 0.431 |
| 0.574 | 0.595 | 0.572 | 0.569 | 0.586 | 0.595 | 0.596 | 0.630 | 0.600 | 0.517 | 0.591 | 0.612 | 0.619 | 0.676 | 0.617 | 0.554 |
| 0.013 | 0.015 | 0.009 | 0.009 | 0.008 | 0.010 | 0.010 | 0.009 | 0.007 | 0.018 | 0.010 | 0.007 | 0.007 | 0.005 | 0.006 | 0.010 |
| 0.008 | 0.009 | 0.010 | 0.007 | 0.008 | 0.008 | 0.007 | 0.010 | 0.011 | 0.009 | 0.007 | 0.009 | 0.011 | 0.011 | 0.007 | 0.011 |
| 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 |
| 0.58 | 0.60 | 0.58 | 0.57 | 0.59 | 0.60 | 0.60 | 0.64 | 0.61 | 0.53 | 0.60 | 0.62 | 0.62 | 0.68 | 0.62 | 0.56 |
| 0.78 | 0.75 | 0.79 | 0.69 | 0.68 | 0.62 | 0.64 | 0.62 | 0.59 | 0.82 | 0.70 | 0.58 | 0.59 | 0.59 | 0.63 | 0.68 |
| 0.01 | 0.01 | 0.01 | 0.00 | 0.02 | 0.03 | 0.02 | 0.04 | 0.05 | 0.00 | 0.02 | 0.03 | 0.04 | 0.05 | 0.03 | 0.01 |
| 0.22 | 0.25 | 0.21 | 0.31 | 0.31 | 0.37 | 0.35 | 0.36 | 0.39 | 0.18 | 0.29 | 0.40 | 0.39 | 0.39 | 0.36 | 0.32 |
| 11.70 | 12.36 | 11.50 | 13.51 | 13.66 | 14.60 | 14.26 | 14.54 | 14.94 | 10.39 | 13.30 | 15.10 | 14.98 | 14.93 | 14.44 | 13.69 |
| 0.45 | 0.77 | 0.44 | 0.50 | 0.50 | 0.49 | 0.52 | 0.45 | 0.31 | 0.53 | 0.49 | 0.53 | 0.50 | 0.40 | 0.41 | 0.44 |
| 0.42 | 0.40 | 0.42 | 0.43 | 0.41 | 0.40 | 0.40 | 0.36 | 0.39 | 0.47 | 0.40 | 0.38 | 0.38 | 0.32 | 0.38 | 0.44 |
| 1.04 | 0.99 | 1.04 | 1.17 | 1.15 | 1.26 | 1.18 | 1.11 | 1.33 | 1.23 | 1.12 | 1.23 | 1.23 | 1.02 | 1.12 | 1.26 |
| 32.46 | 29.85 | 33.03 | 29.56 | 27.67 | 24.27 | 25.43 | 22.26 | 22.62 | 38.92 | 28.15 | 22.05 | 21.69 | 18.49 | 23.73 | 29.64 |
| 45.17 | 44.88 | 45.45 | 39.66 | 39.94 | 36.52 | 38.29 | 39.06 | 35.12 | 43.23 | 41.42 | 35.51 | 36.13 | 39.69 | 38.85 | 38.08 |
| 9.26 | 10.01 | 8.96 | 13.08 | 12.98 | 15.09 | 14.11 | 13.53 | 15.75 | 8.35 | 11.97 | 15.75 | 15.17 | 12.72 | 13.80 | 13.95 |
| 12.89 | 15.05 | 12.33 | 17.55 | 18.74 | 22.71 | 21.25 | 23.74 | 24.45 | 9.27 | 17.62 | 25.36 | 25.28 | 27.31 | 22.59 | 17.93 |
| 0.21 | 0.20 | 0.24 | 0.16 | 0.67 | 1.42 | 0.92 | 1.41 | 2.06 | 0.22 | 0.84 | 1.33 | 1.72 | 1.79 | 1.04 | 0.40 |
| MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr |

| LB 4_18 | LB 4_19 | LB 4_20 | LB 4_21 | LB 4_22 | LB 4_23 | LB 4_24 | LB 4_25 | LB 4_26 | LB 4_27 | LB 4_28 | LB 4_29 | LB 4_30 | LB 4_31 | LB 4_32 | LB 4_33 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 62.45 | 50.97 | 50.48 | 45.93 | 50.72 | 56.83 | 44.72 | 53.73 | 48.97 | 47.84 | 48.97 | 65.21 | 55.11 | 46.83 | 44.35 | 49.96 |
| 8.74 | 17.72 | 18.84 | 22.66 | 19.05 | 14.39 | 21.47 | 16.77 | 19.74 | 19.24 | 19.64 | 6.05 | 15.05 | 21.27 | 22.20 | 19.81 |
| 0.27 | 0.25 | 0.27 | 0.35 | 0.28 | 0.27 | 0.31 | 0.37 | 0.25 | 0.26 | 0.31 | 0.39 | 0.33 | 0.25 | 0.24 | 0.28 |
| 18.21 | 16.82 | 17.75 | 16.76 | 16.02 | 15.88 | 19.23 | 16.10 | 18.19 | 19.22 | 17.95 | 18.52 | 17.05 | 16.57 | 18.14 | 16.94 |
| 9.89 | 14.25 | 12.26 | 13.69 | 13.30 | 12.09 | 13.89 | 12.56 | 12.74 | 13.07 | 12.80 | 9.43 | 12.31 | 15.01 | 14.35 | 12.52 |
| 0.42 | 0.34 | 0.23 | 0.31 | 0.40 | 0.30 | 0.37 | 0.41 | 0.26 | 0.31 | 0.28 | 0.45 | 0.25 | 0.34 | 0.42 | 0.24 |
| 0.26 | 0.32 | 0.39 | 0.47 | 0.43 | 0.34 | 0.45 | 0.32 | 0.46 | 0.36 | 0.39 | 0.48 | 0.19 | 0.50 | 0.47 | 0.50 |
| 100.24 | 100.66 | 100.22 | 100.17 | 100.20 | 100.09 | 100.44 | 100.26 | 100.61 | 100.30 | 100.35 | 100.53 | 100.29 | 100.77 | 100.17 | 100.24 |
| 1.638 | 1.243 | 1.248 | 1.108 | 1.244 | 1.435 | 1.079 | 1.337 | 1.198 | 1.172 | 1.201 | 1.732 | 1.383 | 1.120 | 1.066 | 1.228 |
| 0.342 | 0.644 | 0.694 | 0.815 | 0.697 | 0.542 | 0.772 | 0.622 | 0.720 | 0.703 | 0.718 | 0.240 | 0.563 | 0.758 | 0.795 | 0.726 |
| 0.007 | 0.006 | 0.006 | 0.008 | 0.006 | 0.006 | 0.007 | 0.009 | 0.006 | 0.006 | 0.007 | 0.010 | 0.008 | 0.006 | 0.005 | 0.006 |
| 0.007 | 0.101 | 0.045 | 0.062 | 0.046 | 0.010 | 0.136 | 0.024 | 0.071 | 0.113 | 0.067 | 0.009 | 0.039 | 0.111 | 0.128 | 0.033 |
| 0.499 | 0.333 | 0.419 | 0.366 | 0.370 | 0.414 | 0.355 | 0.400 | 0.400 | 0.385 | 0.398 | 0.512 | 0.414 | 0.308 | 0.333 | 0.407 |
| 0.489 | 0.655 | 0.572 | 0.623 | 0.615 | 0.576 | 0.632 | 0.589 | 0.588 | 0.604 | 0.592 | 0.472 | 0.582 | 0.677 | 0.650 | 0.580 |
| 0.012 | 0.009 | 0.006 | 0.008 | 0.011 | 0.008 | 0.010 | 0.011 | 0.007 | 0.008 | 0.007 | 0.013 | 0.007 | 0.009 | 0.011 | 0.006 |
| 0.007 | 0.008 | 0.010 | 0.012 | 0.011 | 0.009 | 0.011 | 0.008 | 0.011 | 0.009 | 0.010 | 0.013 | 0.005 | 0.012 | 0.011 | 0.013 |
| 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 |
| 0.50 | 0.66 | 0.58 | 0.63 | 0.62 | 0.58 | 0.64 | 0.60 | 0.60 | 0.61 | 0.60 | 0.48 | 0.58 | 0.69 | 0.66 | 0.59 |
| 0.83 | 0.66 | 0.64 | 0.58 | 0.64 | 0.73 | 0.58 | 0.68 | 0.62 | 0.63 | 0.63 | 0.88 | 0.71 | 0.60 | 0.57 | 0.63 |
| 0.00 | 0.05 | 0.02 | 0.03 | 0.02 | 0.01 | 0.07 | 0.01 | 0.04 | 0.06 | 0.03 | 0.00 | 0.02 | 0.06 | 0.06 | 0.02 |
| 0.17 | 0.32 | 0.35 | 0.41 | 0.35 | 0.27 | 0.39 | 0.31 | 0.36 | 0.35 | 0.36 | 0.12 | 0.28 | 0.38 | 0.40 | 0.37 |
| 10.26 | 13.95 | 14.27 | 15.23 | 14.33 | 12.86 | 14.95 | 13.66 | 14.51 | 14.38 | 14.49 | 8.34 | 13.10 | 14.90 | 15.13 | 14.53 |
| 0.39 | 0.36 | 0.39 | 0.47 | 0.40 | 0.39 | 0.43 | 0.50 | 0.37 | 0.38 | 0.44 | 0.52 | 0.45 | 0.37 | 0.35 | 0.40 |
| 0.50 | 0.34 | 0.42 | 0.37 | 0.38 | 0.42 | 0.36 | 0.40 | 0.40 | 0.39 | 0.40 | 0.52 | 0.42 | 0.31 | 0.34 | 0.41 |
| 1.38 | 1.01 | 1.30 | 1.16 | 1.08 | 1.10 | 1.26 | 1.11 | 1.28 | 1.29 | 1.26 | 1.39 | 1.16 | 1.00 | 1.16 | 1.24 |
| 41.70 | 21.82 | 26.91 | 21.07 | 23.85 | 30.30 | 20.43 | 27.47 | 24.92 | 23.79 | 24.84 | 45.58 | 29.27 | 18.32 | 18.95 | 25.74 |
| 40.90 | 42.89 | 36.71 | 35.87 | 39.69 | 42.14 | 36.37 | 40.45 | 36.62 | 37.30 | 36.88 | 42.07 | 41.21 | 40.23 | 37.02 | 36.67 |
| 8.70 | 11.31 | 14.98 | 15.50 | 13.35 | 11.44 | 14.61 | 12.78 | 14.98 | 14.26 | 14.85 | 6.30 | 11.92 | 12.40 | 14.14 | 15.21 |
| 8.53 | 22.22 | 20.43 | 26.38 | 22.22 | 15.90 | 26.02 | 18.82 | 22.01 | 22.36 | 22.05 | 5.82 | 16.78 | 27.24 | 27.62 | 21.68 |
| 0.17 | 1.77 | 0.98 | 1.18 | 0.88 | 0.22 | 2.57 | 0.48 | 1.47 | 2.29 | 1.38 | 0.23 | 0.82 | 1.82 | 2.28 | 0.70 |
| Chr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | Chr | MgChr | MgChr | MgChr | MgChr |

| LB 4_34 | LB 4_35 | LB 4_36 | LB 4_37 | LB 4_38 | LB 4_39 | LB 4_40 | LB 4_41 | LB 4_42 | LB 4_43 | LB 4_44 | LB 4_45 | LB 4_46 | LB 4_47 | LB 4_48 | LB 4_49 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 56.03 | 46.67 | 61.58 | 48.65 | 52.95 | 51.30 | 52.93 | 50.07 | 52.22 | 52.74 | 50.77 | 53.29 | 53.75 | 53.49 | 54.88 | 54.06 |
| 14.29 | 20.62 | 9.86 | 19.21 | 17.44 | 17.66 | 15.80 | 19.75 | 17.59 | 17.79 | 18.85 | 17.66 | 17.60 | 17.24 | 16.14 | 16.73 |
| 0.37 | 0.24 | 0.36 | 0.36 | 0.37 | 0.36 | 0.37 | 0.37 | 0.33 | 0.35 | 0.38 | 0.42 | 0.32 | 0.34 | 0.30 | 0.33 |
| 17.82 | 17.83 | 17.35 | 17.71 | 15.77 | 17.65 | 16.15 | 16.11 | 16.52 | 17.25 | 16.65 | 15.07 | 15.89 | 15.84 | 15.72 | 15.95 |
| 11.05 | 14.06 | 10.92 | 13.53 | 13.05 | 12.38 | 14.12 | 13.05 | 12.87 | 11.59 | 12.78 | 13.04 | 12.42 | 12.88 | 12.39 | 12.53 |
| 0.41 | 0.33 | 0.25 | 0.36 | 0.31 | 0.41 | 0.49 | 0.29 | 0.39 | 0.32 | 0.33 | 0.33 | 0.29 | 0.34 | 0.36 | 0.33 |
| 0.36 | 0.38 | 0.27 | 0.24 | 0.49 | 0.39 | 0.32 | 0.42 | 0.37 | 0.38 | 0.40 | 0.38 | 0.35 | 0.36 | 0.41 | 0.34 |
| 100.33 | 100.13 | 100.60 | 100.06 | 100.37 | 100.14 | 100.18 | 100.06 | 100.29 | 100.43 | 100.17 | 100.19 | 100.62 | 100.49 | 100.19 | 100.29 |
| 1.422 | 1.131 | 1.591 | 1.191 | 1.308 | 1.274 | 1.308 | 1.229 | 1.292 | 1.314 | 1.251 | 1.318 | 1.331 | 1.323 | 1.372 | 1.346 |
| 0.541 | 0.745 | 0.380 | 0.701 | 0.642 | 0.654 | 0.582 | 0.722 | 0.648 | 0.661 | 0.692 | 0.651 | 0.650 | 0.636 | 0.602 | 0.621 |
| 0.009 | 0.006 | 0.009 | 0.008 | 0.009 | 0.008 | 0.009 | 0.009 | 0.008 | 0.008 | 0.009 | 0.010 | 0.008 | 0.008 | 0.007 | 0.008 |
| 0.019 | 0.112 | 0.011 | 0.091 | 0.032 | 0.056 | 0.092 | 0.032 | 0.044 | 0.009 | 0.038 | 0.011 | 0.005 | 0.025 | 0.013 | 0.018 |
| 0.460 | 0.345 | 0.463 | 0.368 | 0.380 | 0.408 | 0.330 | 0.387 | 0.388 | 0.446 | 0.396 | 0.383 | 0.411 | 0.389 | 0.403 | 0.402 |
| 0.529 | 0.643 | 0.532 | 0.625 | 0.608 | 0.580 | 0.658 | 0.604 | 0.600 | 0.544 | 0.594 | 0.608 | 0.580 | 0.601 | 0.584 | 0.588 |
| 0.011 | 0.009 | 0.007 | 0.009 | 0.008 | 0.011 | 0.013 | 0.008 | 0.010 | 0.009 | 0.009 | 0.009 | 0.008 | 0.009 | 0.010 | 0.009 |
| 0.009 | 0.009 | 0.007 | 0.006 | 0.012 | 0.010 | 0.008 | 0.011 | 0.009 | 0.010 | 0.010 | 0.010 | 0.009 | 0.009 | 0.010 | 0.009 |
| 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 | 3.000 |
| 0.54 | 0.65 | 0.53 | 0.63 | 0.62 | 0.59 | 0.67 | 0.61 | 0.61 | 0.55 | 0.60 | 0.61 | 0.59 | 0.61 | 0.59 | 0.59 |
| 0.72 | 0.60 | 0.81 | 0.63 | 0.67 | 0.66 | 0.69 | 0.63 | 0.67 | 0.67 | 0.64 | 0.67 | 0.67 | 0.68 | 0.70 | 0.68 |
| 0.01 | 0.06 | 0.01 | 0.05 | 0.02 | 0.03 | 0.05 | 0.02 | 0.02 | 0.00 | 0.02 | 0.01 | 0.00 | 0.01 | 0.01 | 0.01 |
| 0.27 | 0.37 | 0.19 | 0.35 | 0.32 | 0.33 | 0.29 | 0.36 | 0.33 | 0.33 | 0.35 | 0.33 | 0.33 | 0.32 | 0.30 | 0.31 |
| 12.83 | 14.74 | 10.89 | 14.37 | 13.87 | 13.93 | 13.35 | 14.52 | 13.91 | 13.97 | 14.27 | 13.93 | 13.91 | 13.81 | 13.46 | 13.65 |
| 0.50 | 0.36 | 0.49 | 0.49 | 0.50 | 0.49 | 0.50 | 0.50 | 0.46 | 0.48 | 0.52 | 0.55 | 0.45 | 0.46 | 0.42 | 0.46 |
| 0.46 | 0.35 | 0.47 | 0.37 | 0.38 | 0.41 | 0.33 | 0.39 | 0.39 | 0.45 | 0.40 | 0.39 | 0.41 | 0.39 | 0.41 | 0.41 |
| 1.34 | 1.14 | 1.21 | 1.16 | 1.06 | 1.25 | 0.95 | 1.13 | 1.12 | 1.32 | 1.17 | 1.02 | 1.13 | 1.07 | 1.09 | 1.11 |
| 33.54 | 20.62 | 37.45 | 22.93 | 25.63 | 26.97 | 22.73 | 24.43 | 25.90 | 29.88 | 25.56 | 25.81 | 27.86 | 26.41 | 28.32 | 27.69 |
| 38.59 | 38.43 | 43.06 | 38.92 | 41.01 | 38.33 | 45.36 | 38.15 | 40.08 | 36.52 | 38.32 | 40.98 | 39.27 | 40.79 | 41.02 | 40.49 |
| 12.75 | 13.58 | 8.94 | 13.50 | 12.59 | 13.84 | 10.11 | 14.36 | 13.00 | 15.03 | 14.14 | 12.75 | 13.60 | 12.69 | 12.42 | 12.78 |
| 14.67 | 25.31 | 10.28 | 22.91 | 20.14 | 19.67 | 20.19 | 22.43 | 20.12 | 18.36 | 21.20 | 20.24 | 19.17 | 19.60 | 17.99 | 18.68 |
| 0.45 | 2.05 | 0.27 | 1.75 | 0.63 | 1.18 | 1.61 | 0.63 | 0.89 | 0.20 | 0.78 | 0.22 | 0.10 | 0.51 | 0.26 | 0.37 |
| MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr | MgChr |

| LB 4_50 | LB 4_51 | LB 4_52 | LB 4_53 |
| --- | --- | --- | --- |
| 51.38 | 51.20 | 55.41 | 52.88 |
| 17.86 | 17.37 | 15.86 | 17.40 |
| 0.30 | 0.25 | 0.31 | 0.28 |
| 16.38 | 16.82 | 15.83 | 16.15 |
| 13.76 | 13.88 | 12.34 | 13.03 |
| 0.35 | 0.37 | 0.26 | 0.32 |
| 0.38 | 0.39 | 0.36 | 0.38 |
| 100.41 | 100.29 | 100.38 | 100.43 |
| 1.260 | 1.258 | 1.385 | 1.306 |
| 0.653 | 0.636 | 0.591 | 0.641 |
| 0.007 | 0.006 | 0.007 | 0.006 |
| 0.073 | 0.094 | 0.009 | 0.040 |
| 0.352 | 0.343 | 0.409 | 0.382 |
| 0.636 | 0.643 | 0.582 | 0.607 |
| 0.009 | 0.010 | 0.007 | 0.008 |
| 0.010 | 0.010 | 0.009 | 0.009 |
| 3.000 | 3.000 | 3.000 | 3.000 |
| 0.64 | 0.65 | 0.59 | 0.61 |
| 0.66 | 0.66 | 0.70 | 0.67 |
| 0.04 | 0.05 | 0.00 | 0.02 |
| 0.33 | 0.32 | 0.30 | 0.32 |
| 13.99 | 13.85 | 13.37 | 13.85 |
| 0.42 | 0.36 | 0.44 | 0.40 |
| 0.36 | 0.35 | 0.41 | 0.39 |
| 1.03 | 1.03 | 1.10 | 1.08 |
| 23.15 | 22.71 | 28.90 | 25.71 |
| 41.84 | 42.57 | 41.06 | 40.85 |
| 11.99 | 11.49 | 12.33 | 12.61 |
| 21.68 | 21.53 | 17.52 | 20.04 |
| 1.34 | 1.70 | 0.19 | 0.79 |
| MgChr | MgChr | MgChr | MgChr |