Table S1: Instrument parameters and analytical conditions of LA ICP-MS analyses

| Laser ablation | RESOlution |
| --- | --- |
| Wavelength: | 193 nm (ArF) |
| Pulse length (ns) | 20 |
| Sample cell | Double volume S155 |
| Fluence at sample (J/cm2) | c. 6 |
| Repetition rate (Hz) | 10 |
| Spot size (µm) | 40 |
| Stage speed (mm/min) | 0.5 |
| Ablation mode | Line scan |
| Mass spectrometer | Agilent 8900 |
| RF power (W) | 1400 |
| Sample gas Ar flow (L/min) | c. 0.9 |
| Cool gas Ar flow (L/min) | 13 |
| Auxiliary gas Ar flow (L/min) | c. 0.9 |
| Nitrogen flow (mL/min) | c. 5 |
| He flow (L/min) | c. 0.3 |
| Washout time | 60 s |
| Dwell time | 10 ms |